SealMaster Pavement Products & Equipment	January 2020

PO Box 2277

2520 South Campbell Street

Sandusky, Ohio 44870

Toll Free	800-395-7325

Website	www.sealmaster.net

E-mail	spec@sealmaster.net

Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice, Fifth Edition.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all “Specifier Notes” after editing this section.

Section numbers are from MasterFormat 1995 Edition, with section numbers from MasterFormat 2004 Edition in parentheses.  Delete version not required.

SECTION (32 01 13.62)

BICYCLE LANE TEXTURED COATING SYSTEM

Specifier Notes:  This section covers SealMaster Bicycle Lane Textured Coating System.  Consult SealMaster for assistance in editing this section for the specific application.

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Bicycle Lane Textured Coating System.

1.2	RELATED REQUIREMENTS

Specifier Notes:  Edit the following list of related sections as required.  Delete related sections not required.  List other sections with work directly related to this section.

1.3	REFERENCE STANDARDS

Specifier Notes:  List reference standards mentioned in this section, complete with designations and titles.  Delete reference standards not included in this edited section.  This article does not require compliance with reference standards, but is merely a listing of those used.

A.	U.S. Department of Transportation (MUTCD – Manual on Uniform Traffic Control Devices)

B.	NACTO (National Association of City Transportation Officials)

1.4	SUBMITTALS

A.	Comply with Section 01330 (01 33 00) – Submittal Procedures.

B.	Product Data:  Submit manufacturer’s product data, including surface and crack preparation and application instructions.

C.	Samples:  Submit manufacturer’s color samples of bike lane coating system.

D.	Manufacturer’s Certification:  Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

E.	Warranty Documentation:  Submit manufacturer’s standard warranty.

1.5	QUALITY ASSURANCE

A.	Manufacturer’s Qualifications:

1.	Manufacturer regularly engaged, for past 5 years, in manufacture of textured color coatings for asphalt and concrete substrates.

2.	United States owned company.

B.	Applicator's Qualifications:

1.	Applicator regularly engaged, for past 3 years, in application of specialized pavement coatings of similar scope.

2.	Employ persons trained for application of colored pavement coatings.

1.6	DELIVERY, STORAGE, AND HANDLING

A.	Delivery and Acceptance Requirements:  Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.  Retain all manufacturer batch numbers on each container, in case of future warranty claims.

B.	Storage and Handling Requirements:

1.	Store and handle materials in accordance with manufacturer’s instructions.

2.	Keep materials in manufacturer’s original, unopened containers and packaging until application.

3.	Store materials in clean, dry area indoors.

4.	Store materials out of direct sunlight.

5.	Keep materials from freezing.

6.	Protect materials during storage, handling, and application to prevent contamination or damage.

7.	Close containers when not in use.

1.7	AMBIENT CONDITIONS

A.	Do not apply bicycle lane textured coating system when air or surface temperatures are below 50 degrees F (10 C) during application or within 24 hours after application.

B.	Do not apply bicycle lane textured coating system when rain is expected during application or within 24 hours after application.

PART 2	PRODUCTS

2.1	MANUFACTURER

- SealMaster Pavement Products & Equipment,  PO Box 2277, 2520 South Campbell Street, Sandusky, Ohio   44870.  Toll Free 800-395-7325. Website www.sealmaster.net.  E-mail spec@sealmaster.net.

All other brands must be pre-approved by the architect/engineer, prior to the bid date.  If submitting another brand, bidder must furnish copies of all submittal documents under section 1.4

2.2	MATERIALS

A.	Bicycle Lane Textured Coating System:  Safe Ride Bicycle Lane Coating.

B.	Crack Filler (Ready to Use):  SealMaster “Acrylic Crack Patch”.

1.	100 percent acrylic emulsion trowel-grade crack filler.

2.	Fills cracks in asphalt pavement up to 1 inch wide.

3.	Chemical Characteristics, by Weight, Minimum:

a.	Acrylic Emulsion:  10.0 percent.

b.	Hiding Pigment:  0.2 percent.

c.	Mineral Inert Fillers:  78.0 percent.

d.	Film Formers, Additives:  1.8 percent.

e.	Water:  8.5 percent.

4.	Weight per Gallon at 77 Degrees F:  15.2 lbs., plus or minus 1.0 lbs.

5.	Non-Volatile Material:  80 percent, plus or minus 5 percent.

6.	Color:  [Green]  [Neutral]  [Red].

C.	Surface & Crack Repair:  SealMaster “Acrylic Patch Binder”.

1.	100 percent acrylic emulsion liquid binder.

2.	Mix on-site with sand and cement.

3.	Levels and repairs cracks, surface damage, and depressions up to 3/4 inch deep in pavement.

4.	Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

D.	Bicycle Lane Coating:  Safe Ride Bicycle Lane Coating

1.	Cross-linking Acrylic Polymer Emulsion

2.	Single component, Ready-to-Apply product.

3.	Durable textured pavement color coating for safe, non-slip delineation of bicycle lanes.

4.	Meets the MUTCD requirements for green color night and daytime chromaticity ratings.

5.      Weight per Gallon:  13.5 lbs., plus or minus 0.5 lbs.

6.      Dry mil thickness per coat: 20 to 25 mils.

7.	Color:  Bicycle Lane Green (Safe Ride) – Other colors available upon request.

#### E.	Clear Coat:  ColorPave HD Clear Coat

##### 1.	100% acrylic emulsion

##### 2.	Single component, Ready-to-Apply product.

##### 3.	Provides extra protection from UV, moisture, oil, gas & chemicals.

##### 4.	Dries clear

##### 5.      Weight per Gallon:  8.5 lbs.

##### 6.	Helps to minimize tire marks and enhances green color.

F.	Line Paint:  SealMaster Liquid Thermoplastic Traffic Paint

1.	Pigmented, 100 percent acrylic emulsion line paint.

2.	Line marking on asphalt, concrete, and acrylic surfaces.

3.	Chemical Characteristics, by Weight, Nominal:

a.	Solids:  77.5 percent.

b.	Pigment:  61-62 percent.

4.	Weight per Gallon at 77 Degrees F:  14 lbs., plus or minus 0.75 lbs.

5.	Dry time for no pickup: <6 min

6.	VOC’s:  Less than 100 g/l

7.	Color:  [White] [Yellow] [Blue] [Red]

PART 3	EXECUTION

3.1	EXAMINATION

A.	Examine pavement surface to receive bicycle lane textured coating system.

B.	Notify Architect/Engineer of conditions that would adversely affect application or subsequent use.

C.	Do not begin surface preparation or application until unacceptable conditions are corrected.

3.2	SURFACE PREPARATION

A.	Protection of In-Place Conditions:  Protect adjacent surfaces and landscaping from contact with bicycle lane textured coating system. Masking paper or protective shields may be used to prevent overspray.

B.	Prepare surfaces in accordance with manufacturer’s instructions.

C.	Cure new asphalt surfaces a minimum of 14 to 30 days before application of bicycle lane textured coating system.

D.	Remove dirt, dust, debris, oil, grease, vegetation, loose materials, and other surface contaminants which could adversely affect application of bicycle lane textured coating system.

E.	Repair cracks and surface defects in accordance with manufacturer’s instructions before application of bicycle lane textured coating system.

F.	Ensure surface repairs are flush and smooth to adjoining surfaces.

3.3	APPLICATION

A.	Apply bicycle lane textured coating system in accordance with manufacturer’s instructions at locations indicated on the Drawings.

B.	Mix materials in accordance with manufacturer’s instructions.

C.	Apply a minimum of 2 coats of bicycle lane textured coating system to prepared surfaces in accordance with manufacturer’s instructions.  A 3rd coat shall be applied in conflict zones and areas with high-wear and power steering traffic (i.e. intersections and prime vehicle traffic areas).

D.	Allow material drying times in accordance with manufacturer’s instructions before applying line and symbol markings or opening completed surface to foot traffic.

3.4	LINE MARKINGS

- Lay out bicycle lane markings in accordance with the engineer:

B.	For maximum durability, apply a wet film thickness of 30-35 mils. Follow manufacturers product data sheet for complete application instructions.

3.5	CLEAR COAT

A.	Apply a minimum of 1 clear coat application, per manufacturer specifications.

3.6	PROTECTION

A.	Allow a minimum of 12 to 24 hours curing time before opening bicycle lane textured coating system to traffic.

B.	Protect applied bicycle lane textured coating system to ensure that, except for normal weathering, coating system will be without damage or deterioration at time of Substantial Completion.

END OF SECTION